## Slide 1
DFT in practice: from simple to advanced functionals
Iurii Timrov & Nicola Colonna
THEOS and NCCR-Marvel
Paul Scherrer Institute and NCCR-Marvel

## Slide 2
Outline
Brief recap on KS-DFT. KS equations, common approximations to the xc energy functional, KS in practice
Exercise 0. Standard DFT: PBE band structure of FCC Silicon
Exercise 1-2. Hybrid DFT: electronic structure of FCC Silicon
Exercise 3-4. Meta-GGA: electronic structure of FCC Silicon and BCC Iron using SCAN

## Slide 3
electrons
interaction
external potential
Kohn-Sham particles
(non-interacting)
effective potential
KS MAPPING
Kohn-Sham DFT

## Slide 4
The exchange and correlation energy functional
LDA: The xc energy density of the inhomogeneous system in r is locally approximated with that of a homogeneous electron gas with density n(r)

## Slide 5
The exchange and correlation energy functional
LDA: The xc energy density of the inhomogeneous system in r is locally approximated with that of a homogeneous electron gas with density n(r)
GGA: include the dependence on the gradient of the density

## Slide 6
The exchange and correlation energy functional
LDA: The xc energy density of the inhomogeneous system in r is locally approximated with that of a homogeneous electron gas with density n(r)
GGA: include the dependence on the gradient of the density
Meta-GGA: include the dependency on the laplacian of the density and kinetic energy density

## Slide 7
The exchange and correlation energy functional
LDA: The xc energy density of the inhomogeneous system in r is locally approximated with that of a homogeneous electron gas with density n(r)
GGA: include the dependence on the gradient of the density
Meta-GGA: include the dependency on the laplacian of the density and kinetic energy density
Hybrid functionals: include a fraction of Fock exchange

## Slide 8
KS-DFT in practice: PW and PP
Wavefunctions are represented in Plane Waves (PW)
Gx
Gy
Only Fourier components compatible with the periodicity of the lattice G=n1b1+n2b2

## Slide 9
KS-DFT in practice: PW and PP
Wavefunctions are represented in Plane Waves (PW)
Gx
Gy
Only Fourier components compatible with the periodicity of the lattice G=n1b1+n2b2
All G vectors with norm smaller than |G|max
|G|max defined by setting a cutoff on the kinetic energy Ecut = ħ2/2π |G|2max
Gmax

## Slide 10
KS-DFT in practice: PW and PP
Wavefunctions are represented in Plane Waves (PW)
Gx
Gy
Only Fourier components compatible with the periodicity of the lattice G=n1b1+n2b2
All G vectors with norm smaller than |G|max
|G|max defined by setting a cutoff on the kinetic energy Ecut = ħ2/2π |G|2max
ecutwfc: QE Input parameter for Ecut
Gmax

## Slide 11
KS-DFT in practice: PW and PP
In a periodic system KS states are Bloch functions
Gx
Gy
Only Fourier components compatible with the periodicity of the primitve cell G=n1b1+n2b2
k belong to the Brillouin zone ( )
All G vectors such that ħ2/2π |k+G|2 < Ecut
Many properties requires integration over the k-points -> BZ sampling (K_POINTS card)
Gmax

## Slide 12
KS-DFT in practice: PW and PP
The use of pseudo-potentials allows to ignore chemically inert core electrons and make PW calculation feasible
Strong oscillations close to the nuclei: large number of PW needed

## Slide 13
KS-DFT in practice: PW and PP
The use of pseudo-potentials allows to ignore chemically inert core electrons and make PW calculation feasible
Strong oscillations close to the nuclei: large number of PW needed
Replace the coulombic potetial with a pseudo-potential that produces smooth pseudo-wavefunctions
Different recepies: Norm-conserving, Ultra-soft, Projector-augmented-wave (PAW)

## Slide 14
Where to find PPs
Standard solid-state pseudopotentials (SSSP):
https://www.materialscloud.org/discover/sssp/table/efficiency

## Slide 15
Where to find PPs
Standard solid-state pseudopotentials (SSSP):
https://www.materialscloud.org/discover/sssp/table/efficiency
Quantum Espresso Website:
https://www.quantum-espresso.org/pseudopotentials/
Optimized Norm-Conserving Vanderbilt (ONCV): SG15
http://www.quantum-simulation.org/potentials/sg15_oncv/
Optimized Norm-Conserving Vanderbilt (ONCV): pseudo-dojo
http://www.pseudo-dojo.org/

## Slide 16
Outline
Brief recap on KS-DFT. KS equations ad common approximations to the xc energy functional, KC in practice
Exercise 0. Standard DFT: PBE band structure of FCC Silicon
Exercise 1-2. Hybrid DFT: electronic structure of FCC Silicon
Exercise 3-4. Meta-GGA: electronic structure of FCC Silicon and BCC Iron using SCAN

## Slide 17
FCC Silicon
a3
a1
a2
a0
y
z
Goal of exercise0

## Slide 18
Silicon PBE electronic structure: SCF calculation
&control
calculation='scf'
prefix='Si'
pseudo_dir = '../../files/pseudo'
outdir='./out'
/
&system
ibrav = 2, celldm(1) = 10.262,
nat = 2, ntyp = 1,
ecutwfc = xxx ,
/
&electrons
conv_thr = 1.d-8
/
ATOMIC_SPECIES
Si 28.086 Si.pbe_PseudoDojo.UPF
ATOMIC_POSITIONS {alat}
Si 0.00 0.00 0.00
Si 0.25 0.25 0.25
K_POINTS {automatic}
XXX YYY ZZZ 0 0 0
Self-consistent field calculation
Directory conatining the PPs
Temporary files re stored here
Specify here the crystal structure:
FCC, alat=10.20 Bohr, 2 Si atoms
Cutoff for the Wave-Functions
Convergence threshold for the SCF problem
https://www.quantum-espresso.org/Doc/INPUT_PW.html
BZ sampling
Pseudopotetial file
Atomic positions
a3
a1
a2
a0
y
z

## Slide 19
Convergence wrt ecut: total energy

## Slide 20
Convergence wrt ecut: direct band gap

## Slide 21
Convergence wrt ecut: indirect band gap

## Slide 22
Convergence wrt K_POINTS: total energy

## Slide 23
Convergence wrt K_POINTS: direct band gap

## Slide 24
Check-out the git repo
The hands-on materials are available at github
Clone the repository (or Download it):
  git clone https://github.com/materialscloud-org/hubbard-koopmans-2022
Go to the exercise0 folder
  cd hubbard-koopmans-2022/Day1/exercise0

## Slide 25
Silicon PBE electronic structure: SCF calculation
&control
calculation='scf'
prefix='Si'
outdir='./out'
/
&system
ibrav = 2, celldm(1) = 10.20,
nat = 2, ntyp = 1,
ecutwfc = 40 ,
/
&electrons
conv_thr = 1.d-8
/
ATOMIC_SPECIES
Si 28.086 Si.pbe_PseudoDojo.UPF
ATOMIC_POSITIONS {alat}
Si 0.00 0.00 0.00
Si 0.25 0.25 0.25
K_POINTS {automatic}
12 12 12 0 0 0
Converged value for the Wave-Functions cutoff
https://www.quantum-espresso.org/Doc/INPUT_PW.html
Converged value for the
BZ sampling

## Slide 26
Silicon PBE electronic structure: BANDS calculation
&control
calculation='bands'
...
/
&system
...
/
&electrons
...
/
ATOMIC_SPECIES
...
ATOMIC_POSITIONS {alat}
...
K_POINTS {crystal_b}
5
0.50000 0.50000 0.50000 20 ! L
0.00000 0.00000 0.00000 20 ! G
0.50000 0.00000 0.50000 20 ! X
0.37500 0.37500 0.75000 20 ! K
0.00000 0.00000 0.00000 0 ! G
"Bands" calculation
Number of special k-points provided
Coordinates of the special k-points and number of addditional points QE generates between two adiacent special k-points.
https://www.quantum-espresso.org/Doc/INPUT_PW.html

## Slide 27
PBE Silicon band structure

## Slide 28
PBE Silicon band structure
Egindirect = 0.57 eV
Egdirect = 2.56 eV
 | indirect | direct
Eg Exp.​ | 1.17​ | 3.35​

## Slide 29
Outline
Brief recap on KS-DFT. KS equations, common approximations to the xc energy functional, KS in practice
Exercise 0. Standard DFT: PBE electronic structure of FCC Silicon
Exercise 1-2. Hybrid DFT: electronic structure of FCC Silicon
Exercise 3-4. Meta-GGA: electronic structure of FCC Silicon and BCC Iron using SCAN

## Slide 30
Hybrid functionals
Mix a fraction of exact-exchage from HF theory with semi-local exchage
3-paramenters: combination of x-HF, x-B88(xGGA), c-LYP(cGGA) and xc-LDA
  Fitted on thermochemical data: a0 = 0.20, ax=0.72, ac=0.81
  [Becke et al. JCP 98, 5648 (1993), Stephens et al. J. Phys. Chem. 98, 11623 (1994)]

## Slide 31
Hybrid functionals
Mix a fraction of exact-exchage from HF theory with semi-local exchage
3-paramenters: combination of x-HF, x-B88(xGGA), c-LYP(cGGA) and xc-LDA
  Fitted on thermochemical data: a0 = 0.20, ax=0.72, ac=0.81
  [Becke et al. JCP 98, 5648 (1993), Stephens et al. J. Phys. Chem. 98, 11623 (1994)]
Simplification: ax=(1-a0), ac=1. Only 1 mixing parameter [Becke et al. JCP 104, 1040 (1996)]
    Comparison with 4° order perturbation theory: a0 = 1/4: PBE0 [Perdew et al. JCP 105, 9982 (1996)]

## Slide 32
Range-separated Hybrid functionals
Basic Idea: split the electron-electron interaction in short and long range
b= 0 -> Conventional hybrid functional. E.g. b = 0 and a = 0.25 -> PBE0
a = -b = 0.25 and µ = 0.106 bohr-1 -> HSE
a+b=1 -> correct asymptotic (1/r) in finite systems
a+b=1/ε -> correct asymptotic (1/εr) in extended systems
µ can be tuned to satisfy the IP theorem (Optimal tuning) [Lecture by Prof. Kronik]
Long-Range
Short-Range
Range-separation
parameter

## Slide 33
Exact-exchange energy
In Reciprocal space:
Integration over the BZ: nqx1, nqx2, nqx3
Need to be compatible
with the k mesh
Integrable divergence for q+G->0
exxdiv_treatment=‘gygi-baldereschi’
x_gamma_extrapolation = .true.
PW expansion
ecutfock
Equal to ecutrho by default.
Can be reduced (but not below ecutwfc)

## Slide 34
Silicon PBE0 electronic structure: SCF calculation
&control
...
/
&system
...
input_dft = "pbe0"
nqx1 = XXX, nqx2 = XXX, nqx3 = XXX
exxdiv_treatment = "gb"
x_gamma_extrapolation = .true.
ecutfock = YYY
exx_fraction = ZZZ
screening_parameter = WWW
/
&electrons
...
/
ATOMIC_SPECIES
...
ATOMIC_POSITIONS {alat}
...
K_POINTS {automatic}
12 12 12 0 0 0
https://www.quantum-espresso.org/Doc/INPUT_PW.html
Specify which hybrid functional: PBE0/B3LYP/HSE
You can change the fraction of EXX and/or the
range separation parameter.

## Slide 35
PBE0 energy convergence wrt ecutfock

## Slide 36
PBE0 energy convergence wrt nqx

## Slide 37
PBE0 direct band Gap convergence wrt nqx

## Slide 38
PBE0 indirect band Gap convergence wrt nqx

## Slide 39
Outline
Brief recap on KS-DFT. KS equations, common approximations to the xc energy functional, KS in practice
Exercise 0. Standard DFT: PBE electronic structure of FCC Silicon
Exercise 1-2. Hybrid DFT: electronic structure of FCC Silicon
Exercise 3-4. Meta-GGA: electronic structure of FCC Silicon and BCC Iron using SCAN

## Slide 40
Check-out the git repo
Go to the exercise1 folder
  cd hubbard-koopmans-2022/Day1/exercise1

## Slide 41
Silicon PBE0 electronic structure: SCF calculation
&control
...
/
&system
...
input_dft = "pbe0"
nqx1 = 4, nqx2 = 4, nqx3 = 4
exxdiv_treatment = "gb"
x_gamma_extrapolation = .true.
ecutfock = 40
/
&electrons
...
/
ATOMIC_SPECIES
...
ATOMIC_POSITIONS {alat}
...
K_POINTS {automatic}
12 12 12 0 0 0
Converged parameters for nqx
Converged value for ecutfock

## Slide 42
Nested self-consistent loop
Update VHF
Energy converged?
Converge ρ(r) with fixed VHF
Normal scf (LDA or similar) is performed
Hybrid functional is switched. VHF is calculated using the current best wfcs
A new scf is performed keeping VHF fixed
Exchange error (dexx) is computed
If dexx > thr the procedure is repeated from 1.
NO
YES
Outer-loop
Inner-loop
JOB DONE

## Slide 43
HSE energy convergence wrt nqx

## Slide 44
HSE direct band Gap convergence wrt nqx

## Slide 45
HSE indirect band Gap convergence wrt nqx

## Slide 46
Silicon HSE electronic structure: SCF calculation
&control
...
/
&system
...
input_dft = "hse"
nqx1 = 4, nqx2 = 4, nqx3 = 4
exxdiv_treatment = "gb"
x_gamma_extrapolation = .true.
ecutfock = 40
/
&electrons
...
/
ATOMIC_SPECIES
...
ATOMIC_POSITIONS {alat}
...
K_POINTS {automatic}
12 12 12 0 0 0
Converged parameters for nqx
Converged value for ecutfock

## Slide 47
Silicon band Gap: summary
Functional​ | indirect Gap​ | Direct Gap | Band width
PBE | 0.57 | 2.56 | 11.96
PBE0​ | 1.85 | 4.04 | 13.32
HSE​ | 1.15 | 3.33 | 13.26
Exp. | 1.17 | 3.35 | 12.5
ecut = 40 Ry, k mesh: 12x12x12
ecutfock = 40 Ry, q mesh: 4x4x4

## Slide 48
Hybrids: how do they perform
Functional​ | MAE(G2)​ | MAE(G2-1) | Max AE(G2) | Max AE(G2-1)
LDA | 83.7 | 36.4 | 216 | 84
PBE​ | 17.1 | 8.6 | 52 | 26
BLYP | 7.1 | 4.7 | 28 | 15
B3LYP | 3.1 | 2.4 | 20 | 10
PBE0 | 4.8 | 3.5 | 24 | 10
Atomization energies
Mean Absolute Error (MAE) in Kcal/mol for the G2 (148 molecules)
and G2-1( (55 molecules) sets.
Curtiss et al. JCP 106, 1063 (1997); Scuseria et al. JCP 110, 5029 (1999)

## Slide 49
Hybrids: how do they perform
​ | PBE | PBE0 | HSE | B3LYP
MRE | 0.8 | 0.1 | 0.2 | 1.0
MARE | 1.0 | 0.5 | 0.5 | 1.2
No-metals |  |  |  | 
MRE | 1.0 | 0.0 | 0.1 | 0.8
MARE | 1.0 | 0.4 | 0.5 | 0.8
Lattice constants of solids
Marsman et al. J. Phys: Condens. Matter 20, 064201 (2008)
​ | PBE | PBE0 | HSE | B3LYP
MRE | -9.8 | -1.2 | -3.1 | -10.2
MARE | 9.4 | 5.7 | 6.4 | 11.4
No-metals |  |  |  | 
MRE | -10.4 | -0.7 | -1.8 | -6.8
MARE | 10.4 | 3.8 | 4.6 | 7.4
Bulk modulus of solids

## Slide 50
Hybrids: how do they perform
Band gaps
Heyd et al. JCP 123, 174101 (2005)
Improved band gaps for semiconducting system HSE correctly predict semiconducting behavior in systems where LDA/GGA predicts a metal
Error (in eV) for 40 simple and binary semiconductors and insulators
​ | LDA | PBE | HSE
ME | -1.14 | -1.13 | -0.17
MAE | 1.14 | 1.13 | 0.26

## Slide 51
Caveat
More expensive than standard DFT (time- and memory-wise)
No hybrid PP. Use always a PP generated with the same local functional as the one used in the hybrid functional definition (e.g. use PBE PPs for PBE0 calculations)
NLCC not well defined. Avoid PPs with NLCC
Might need to explicitly include semi-core states electrons in the valence
Calculations with US and PAW PPs typically slower that those with NC PPs
Not all the features are implemented for US and PAW PPs
Wannier interpolation to get the entire band structure (see hnds-on later today)